BORON ULTRA 78 and BORON RODS - PASTE INJECTION + RODS - HOLE DRILLING CALCULATOR

1. INJECTION HOLES - 8MM DIAMETER

2. DEPTH OF HOLES - TO WITHIN 15MM OF OPPOSING FACE

3. HOLES PER METRE - 8

4. SPACING OF HOLES - 120MM ALONG THE GRAIN DIRECTION

- 75MM ACROSS THE GRAIN

METHOD A - DRILLING INTO THE FACE (WIDE SIDE) OF A TIMBER

TIMBER SIZE	HOLE	       ROWS       CC/METRE  	METRES PER

(METRIC)		DEPTH			    RUN        CARTRIDGE (380)

4" X 2"			35mm		1		14			27

(100x50)

5" x 2"			35mm		2		28			14

(125x50)

6" x 2"			35mm		2		28			14

(150x50)

7" x 2"			35mm		2		28			14

(175x50)

8" x 3"			60mm		3		72			5.3

(200x75)

9" x 3"			60mm		3		72			5.3

(225x75)

10" x 3"		60mm		3		72			5.3

(250x75)

12" x 3"		60mm		4		96			4

(300x75)

METHOD B - DRILLING INTO THE EDGE (NARROW SIDE) OF A TIMBER

TIMBER SIZE	HOLE	       ROWS       CC/METRE  	METRES PER

(METRIC)		DEPTH			    RUN        CARTRIDGE (380)

4" X 2"			95mm		1		38			10

(100x50)

5" x 2"			120mm	1		48			7.9

(125x50)

6" x 2"			145mm	1		58			6.6

(150x50)

7" x 2"			170mm	1		68			5.6

(175x50)

8" x 3"			195mm	1		78			4.9

(200x75)

9" x 3"			220mm	1		88			4.3

(225x75)

10" x 3"		245mm	1		98			3.9

(250x75)

12" x 3"		295mm	1		118			3.2

(300x75)

BORON ULTRA 78/RODS - PASTE INJECTION + RODS - HOLE DRILLING PATTERN

METHOD A -  DRILLING INTO THE FACE

120MM SPACING ALONG THE GRAIN - 50MM IN FROM EACH END

O		O		O		O		O		O                   O

2"-3" (50-75mm)

O		O		O		O		O		O                   O

2"-3" (50-75mm)

METHOD B -  DRILLING INTO THE EDGE

120MM SPACING ALONG THE GRAIN - 50MM IN FROM EACH END

METHOD B -  DRILLING INTO THE EDGE

120MM SPACING ALONG THE GRAIN - 50MM IN FROM EACH END

O		O		O		O		O		O

O		O		O		O		O		O		O

O		O		O		O		O		O

O		O		O		O		O		O		O 12"-13"(300-325mm)

O		O		O		O		O		O

O		O		O		O		O		O		O

O		O		O		O		O		O

O		O		O		O		O		O		O 12"-13"(300-325mm)

O		O		O		O		O		O

O		O		O		O		O		O		O

O		O		O		O		O		O

8"-10" (200-250mm)

O		O		O		O		O		O

O		O		O		O		O		O		O

O		O		O		O		O		O

8"-10" (200-250mm)

O		O		O		O		O		O

5"-7" (125-175mm)

O		O		O		O		O		O

O		O		O		O		O		O

5"-7" (125-175mm)

O		O		O		O		O		O

O		O		O		O		O		O

up to 4" (100mm)

O		O		O		O		O		O

up to 4" (100mm)